## Slide 1
Characterizing Early Organic Glass Scintillator Beta-Cell Prototypes for Radioxenon Monitoring
2024 MTV Workshop
March 26
Tessa Maurer
Graduate Student, University of Michigan
E. A. Schneider1, S. D. Clarke1, K. L. Meagher1, P. L. Feng2, S. A. Pozzi1
1University of Michigan
2Sandia National Laboratories

## Slide 2
  Motivation
  Radioxenon indicator of nuclear weapon detonation
    Can measure with beta-gamma coincidence detection system that uses plastic scintillators
  Plastic scintillators can exhibit radioxenon “memory effect”1
  Alternatives like organic stilbenes are expensive and difficult to shape
    Motivation to investigate commercially viable scintillating material with desired properties
Coincidence detector with rounded plastic cell2
  1L. Blackberg, et al., “Investigations of surface coatings to reduce memory effect in plastic scintillator detectors used for radioxenon detection,” NUCL. INSTR. METH. A., vol. 656, no. 1, pp. 84 – 91, 2011. [Online]. Available: http://www.sciencedirect.com/science/article/pii/S0168900211014884
  2Sivels, C.B., et al., ”A review of the developments of radioxenon detectors for nuclear explosion monitoring,” J Radioanal Nucl Chem 314, 829–841 (2017). https://doi.org/10.1007/s10967-017-5489-2
Notes: Beta gamma coincidence system looks for
Rounded beta cell allows for use of 1 PMT, refocusing signal on cap side back towards the readout
State previous work shows stilbene has reduced memory effect, but…

## Slide 3: The Beta-Cell
Beta-cell typically organic scintillator because of efficiency for low energy (<10 MeV) beta particles
The beta-cell contains the gas sample being measured
  ‘Test tube’ shape to improve structural integrity and to redirect signal back into readout
The beta-cell needs to be thin enough to allow gamma rays to escape to the surrounding inorganic gamma cell, but thick enough the detect betas and maintain structural integrity under vacuum
A rounded plastic beta-cell from PNNL3
3C.B. Sivels (2018). Development of an Advanced Radioxenon Detector for Nuclear Explosion Monitoring (Handle: 2027.42/147543) [Doctoral dissertation, University of Michigan, Ann Arbor]. Deep Blue
4Le Petit, G et al. “Innovative concept for a major breakthrough in atmospheric radioactive xenon detection for nuclear explosion monitoring.” Journal of radioanalytical and nuclear chemistry vol. 298,2 (2013): 1159-1169. doi:10.1007/s10967-013-2525-8
Main decay modes of relevant radioisotopes of xenon4

## Slide 4: Project Mission
  We are testing and casting new small-molecule organic glass scintillating (OGS) material*
    Potential substitute of plastic scintillators in beta-cell
    OGS shapeable and has comparable resolution to stilbene scintillators
  We cast and characterized various OGS beta-cell prototypes:
    5-mm thick hollow square cylinder
    2.8-mm thick hollow square cylinder
OGS 4 mm thick slab
  *Developed by Sandia National Laboratories
5-mm thick hollow square OGS cylinder beta-cell prototype with endcaps

## Slide 5: MTV Impact and Mission Relevance
MTV students Leah and Tessa
MTV impact
Project built from collaborations with Sandia National Laboratories
NNSA mission of Nonproliferation and Arms Control
  ”Developing and maintaining the technical means to monitor whether the terms of a nuclear arms control treaty or other international agreement are fulfilled is a critical factor in ensuring that such agreements are successful”
  Characterization of OGS provides valuable insight into this new scintillator’s potential in radioxenon monitoring for treaty verification

## Slide 6: Organic Glass Casting at University of Michigan
5. Wrap OGS in reflective wrapping
3. Pour molten OGS into custom silicone molds and cool gradually in oven for ~14 hours
1. Bulk OGS
4. Polish as needed and apply protective PVA coating
2. Melting and degassing bulk OGS

## Slide 7: Organic Glass Beta-Cell Development
Each OGS beta-cell cast in three pieces: one 3 mm thick solid endcap, one 3 mm thick endcap with gas inlet, and 18 x 41 mm height square hollow cylinder
  OGS material from BlueShift Optics cast
  Square hollow cylinders with thicknesses of 2.8 and 5 mm produced
Glued pieces together with 1:1 polyvinyl alcohol (PVA) to water mixture
MTV graduate fellow Ethan sanding OGS sample
Endcaps for OGS beta-cell
Square hollow OGS cylinders and metal mold negatives

## Slide 8: Pulse Integral Distributions of Assembled Beta-Cell and Individual Parts
Light output distributions measured for (bare) assembled OGS beta-cells and (bare) individual parts
  Measured 137Cs
  Used same 38.1 mm Hamamatsu PMT H3178-51
    Consistent operating voltage of -1350 V

## Slide 9: Characterization Procedure
137Cs can be measured with inorganic and organic detector in coincidence to find relative energy resolution of organic
Outside of OGS beta-cells wrapped in Teflon tape
OGS coupled to 38.1 mm Hamamatsu PMT H3178-51
76.2 mm NaI(Tl) placed just above OGS
OGS beta-cell
NaI
137Cs
130 mm
Compton scattering in OGS
Full deposition in NaI of remaining energy
137Cs coincidence distribution with 25.4 mm diameter OGS cylinder and 76.2 mm diameter NaI(Tl)
  Thinner width of diagonal  better resolution
Notes: Energy resolution determination from organics alone difficult due to dominant Compton scattering interaction
Explain quadrature sum effect

## Slide 10: 137Cs Coincidence Distributions for OGS Beta-Cells
2.8 mm thick OGS beta-cell
5 mm thick OGS beta-cell

## Slide 11: Domed Hollow Cylinder Geometry OGS Beta-Cell
3D printed polyvinyl alcohol mold to produce hollow domed cylinder piece according to ‘test tube’ shapes used in field
  Polyvinyl alcohol is water soluble
    Mold release is water bath, inducing least amount of stress to OGS sample
  3D printed material not smooth, OGS sample may require machining or sanding
CAD models and PVA 3D printed hollow domed cylinder mold (note there is cavity within mold that molten OGS fills)

## Slide 12: Expected Impact
Increased level of radioxenon can be due to variety of reasons, not just nuclear weapon detonation
  Ratio of xenon radioisotopes indicates origins of increase
Improved beta-cell energy resolution  better distinction of key radioxenon isotopes used for event identification
  Higher confidence in International Monitoring System’s reporting violations of the Comprehensive Nuclear Test Ban Treaty
C.B. Sivels (2018). ”Development of an Advanced Radioxenon Detector for Nuclear Explosion Monitoring” (Handle: 2027.42/147543) [Doctoral dissertation, University of Michigan, Ann Arbor]. Deep Blue
P.E. Keller, “Categorization of Radioxenon,” Pacific Northwest National Laboratory, 2012, pnnl.gov/publications/categorization-radioxenon

## Slide 13: Conclusion and Summary
Square hollow cylindrical cells of organic glass have been successfully cast and tested using a 137Cs source
  OGS 2.8 mm and 5 mm thick beta-cells do not have significant differences in energy resolution
    Light transport complexities due to geometry merit further investigation and may be degrading energy resolution
If better performing beta-cells compared to currently deployed plastic scintillators, will support nonproliferation efforts to identify nuclear weapon detonation via radioxenon monitoring

## Slide 14: Next Steps
Use epoxy or thermal coupling to assemble OGS beta-cell pieces instead of PVA and water mixture
Investigate 3D printed water-soluble molds for ‘test tube’ beta-cell geometry
Compare results with simulation and plastic beta-cells
Investigate other geometries and additives such polymers to improve mechanical properties

## Slide 15: Acknowledgements
The Consortium for Monitoring, Technology, and Verification would like to thank the DOE-NNSA for the continued support of these research activities.
  This work was funded by the Consortium for Monitoring, Technology, and Verification under Department of Energy National Nuclear Security Administration award number DE-NA0003920

## Slide 16: Organic Glass Scintillating (OGS) Material
OGS material produced by Sandia National Laboratories5
OGS emits blue light
90:10 mixture of P2 and PB3 with 0.2 wt% bis-MSB wavelength shifter
Can be used in many applications, including imaging (see oral presentation “Visualizing Particle Imaging using the HoloLens 2” Ricardo Lopez)
P2 Molecular Formula: C42H36Si
PB3 Molecular Formula: C51H44Si
5Lucas Q. Nguyen, et al., “Boron-loaded organic glass scintillators,” NUCL. INSTR. METH. A., Volume 988, 2021, 164898, ISSN 0168-9002

## Slide 17: Characterization Procedure (continued)
Outside of OGS beta-cells wrapped in Teflon tape
OGS coupled to 38.1 mm Hamamatsu PMT H3178-51
76.2 mm NaI(Tl) placed just above OGS
137Cs placed 130 mm off axis of center
Diffuse wrapped beta-cell
NaI